## Slide 1: Artificial Photosynthesis
Christina Chang
And Sahad Vasanji
HEJC
5/23/2018

## Slide 2: Photosynthesis
FOOD = FUEL
+
SUNLIGHT
Water
+
+
Oxygen
CO2

## Slide 3: Artificial Photosynthesis
FUEL
+
SUNLIGHT
Water
+
Oxygen
Hydrogen
+ CO2
Carbon-based fuels

## Slide 4: Mimicking Photosynthesis using a “Z-Scheme”
DOI: 10.1038/NPHOTON.2012.175

## Slide 5
DOI: 10.1038/NPHOTON.2012.175
Several structural designs exist for artificial photosynthesis

## Slide 6
DOI: 10.1038/NPHOTON.2012.175

## Slide 7: Technical Challenges in Artificial Photosynthesis
FUEL
+
SUNLIGHT
Water
+
Oxygen
Hydrogen
+ CO2
Carbon-based fuels
Overpotential
And efficiency
Selectivity and Separations
System cost
System robustness/lifetime
Testing standardization
Separations
Is integrated “Artificial Photosynthesis” better than solar PV + H2O electrolysis?
Notes: Highest electrical to power is 64%, molecular foundry, Nature Chemistry 11/20/2017, Univ. Toronto, Edward Sargent and David Prendergast
* CO2 → formate, Nature 2016, 240 mV overpotential by Xu Zhang

## Slide 8
Interfacial engineering of a semiconductor nanoparticle—catalyst system for efficient and stable solar H2 generation in pH neutral water
Christina M. Chang
Reisner Laboratory

## Slide 9
YOUR
FOOTPRINT

## Slide 10
FOOTPRINT
H2
YOUR
chemicals
27%
oil refining
20%
H2 use data: The Essential Chemical Industry, Univ, of York (2016).
fertilizer (NH3)
53%
H2 source data: Global CCS Institute (2008)
natural gas
48%
oil + coal
48%
water electrolysis
4%

## Slide 11
FOOTPRINT
H2
YOUR
chemicals
27%
oil refining
20%
fertilizer (NH3)
53%
solar water splitting
water electrolysis
H2 source data: Global CCS Institute (2008)
H2 use data: The Essential Chemical Industry, Univ, of York (2016).

## Slide 12
hν
Quantum dots can act as photosensitizers for
H2 production catalysts

## Slide 13: There is a lack of QD-based systems operating at neutral pH
Chart: 
| 2 | 2 | 4 | 4.5999999999999996 | 4 | 4.5 | 12 | 7
TON_opt | 2607 | 150 | 505 | 23400 | 27135 | 600000 | 2170 | 58000
H2 produced / catalyst
organic
solvents
pH not
reported
a
b
c
d
e
f
g
h
aqueous pH
a) Huang, J., Chen, L., et al. JACS 2012, 1-5. | e) Li, Z.-J., Wu, L.-Z., et al. EES 2012
b) Wen, F., Li, C., et al. ChemSusChem 2012, 5, 849–853. | f) Han, Z., Krauss, T. D., et al. Science 2012, 338, 1321–4.
c) Wang, F., Wu, L.-Z., et al. ACIE, 2011, 50, 3193–7 | g) Zhao, J., Osterloh, F. E., et al. ACS Nano 2013, 7, 4316–4325
d) Wang, F., Wu, L.-Z., et al. ACIE 2013 | h) Huang, L., Li, C., et al. JPCC 2013

## Slide 14
Dr. Erwin Reisner
Principal Investigator
Christian Doppler Laboratory
Christina Chang
MPhil Student, Marshall Scholar (2012)
Dr. Katherine Orchard
AIMR Joint Research Centre Scientist (2012)
Dr. Benjamin Martindale
PhD Student, E. Oppenheimer Scholar (2012)

## Slide 15
C. M. Chang,* K. L. Orchard,* B. C. M. Martindale, E. Reisner. J. Mater. Chem. A., 2016, 4, 2856.

## Slide 16
Outline
Ligand removal hypothesis
Experimental approach and testing
What is the active catalyst?
C. M. Chang,* K. L. Orchard,* B. C. M. Martindale, E. Reisner. J. Mater. Chem. A., 2016, 4, 2856.

## Slide 17: Hypothesis: ligands are a barrier to the catalytic reaction
pH << 7

## Slide 18: Hypothesis: ligands are a barrier to the catalytic reaction
pH << 7

## Slide 19: Hypothesis: ligands are a barrier to the catalytic reaction
pH << 7
Ligands desorb more readily,
enabling catalysis
hν

## Slide 20: Hypothesis: ligands are a barrier to the catalytic reaction
pH << 7
Ligands desorb more readily,
enabling catalysis
hν
Ligands strongly attached;
catalysis cannot occur
pH ≥ 7
hν

## Slide 21: MPA-capped QDs exhibit no photocatalysis at pH 7
Sample Prep
2.5 mL
QD-MPA (0.05 mL)
CoCl2 (0.05 mL)
Na2SO3 + HCl, pH 7 (2.4 mL)
Purge 10 min with 2% CH4 in N2
2 uM QD-MPA
4 uM CoCl2
0.1 M Na2SO3
2.5 mL
Synthesis
Photocatalytic testing
lamp
100 mW/cm2
AM
1.5 filter
Water filter
-IR
420 nm filter
-UV
water jacket, 25 °C
GC
20 uL
No H2 detected over 4 hrs

## Slide 22: Ligands were removed from CdS QDs
Rosen, E.L., Buonsanti, R., Llordes, A., Sawvel, A.M., Milliron, D.J. and Helms, B.A.. ACIE, 2012. 51(3), pp.684-689.
Mechanism
Procedure

## Slide 23: Ligands were removed from CdS quantum dots without significant changes in structure
5.0 nm
4.2 nm
5.0 nm
Intensity / AU
Absorbance / AU
350
400
450
500
550
Wavelength / nm

## Slide 24: Ligand removal from CdS QDs allows photocatalytic H2 production from pH neutral water

## Slide 25: The catalytic system was optimized
Increasing [Co] helps up to a point
[Na2SO3] is limiting
pH 7 is optimal
Increasing [QD] helps up to a point
Optimal
conditions
H2 / μmol
H2 / μmol
H2 / μmol
H2 / μmol
[QD] / μM
[Na2SO3] / M
[CoCl2] / μM
pH

## Slide 26: Long-term photoactivity of the optimized system is limited by buffering capability of the electron donor

## Slide 27: There is a lack of QD-based systems operating at neutral pH
Chart: 
| 2 | 2 | 4 | 4.5999999999999996 | 4 | 4.5 | 12 | 7
TON_opt | 2607 | 150 | 505 | 23400 | 27135 | 600000 | 2170 | 58000
H2 produced / catalyst
organic
solvents
pH not
reported
a
b
c
d
e
f
g
h
aqueous pH
a) Huang, J., Chen, L., et al. JACS 2012, 1-5. | e) Li, Z.-J., Wu, L.-Z., et al. EES 2012
b) Wen, F., Li, C., et al. ChemSusChem 2012, 5, 849–853. | f) Han, Z., Krauss, T. D., et al. Science 2012, 338, 1321–4.
c) Wang, F., Wu, L.-Z., et al. ACIE, 2011, 50, 3193–7 | g) Zhao, J., Osterloh, F. E., et al. ACS Nano 2013, 7, 4316–4325
d) Wang, F., Wu, L.-Z., et al. ACIE 2013 | h) Huang, L., Li, C., et al. JPCC 2013
this work; EQE 7.7% at 420 nm

## Slide 28
20 nm
Ligand-stripped QDs aggregate in water

## Slide 29
5 nm
Ligand-stripped QDs retain nanocrystallinity
CdS

## Slide 30
QD aggregates isolated from solution retain activity,
confirming Co is attached

## Slide 31
Co may be attached to the QDs in several possible ways
Surface attachment is most likely, either as:
a known active catalyst (e.g. CoXSy or CoxOy)
adsorbed Co2+ ions (e.g. at OH- or SOx2- sites) which could promote CdS catalytic ability or trap charges to increase charge separation
known
active catalyst (lit).
adsorbed Co2+

## Slide 32
Conclusions
Ligand stripping is an easy and effective method to activate QDs in photocatalytic schemes
This method afforded a QD/Co hybrid system with unprecedented photoactivity in pH neutral solution
The system performs for (at least) several days, limited by the buffering ability of the electron donor
The active system is bare CdS QDs with an attached cobalt species to enhance catalysis

## Slide 33
OUR
FOOTPRINT

## Slide 34
Acknowledgements & Funding
Ernest
Oppenheimer Fund
Prof. Erwin Reisner
Dr. Katherine Orchard
Benjamin Martindale
Dr. Fezile Lakadamyali
Dr. Moritz Kuehnel
Dr. Micaela Crespo
Collaborators
Prof. James Durrant
Dr. Anna Reynal-Verdu
Dr. Mahmoud Adrakani

## Slide 35
C. M. Chang,* K. L. Orchard,* B. C. M. Martindale, E. Reisner. J. Mater. Chem. A., 2016, 4, 2856.