## Slide 1
Andrew Wong – Harvard Energy Journal Club – 3 April 2019
Recovering
Electrochemical
Components and
Yielding
Cathodes while
Lowering
Emissions

## Slide 2: The need for better batteries
Yoo et al. Materials Today, 2014, 17, 3
DOI: 10.1016/j.mattod.2014.02.014

## Slide 3: Some major battery chemistries
Alkaline batteries
  Zn/KOH/MnO2
Lead-acid
  Pb/H2SO4/PbO2
NiCad
  Cd/KOH/Ni(OH)2
Nickel metal hydride
  MH/KOH/Ni(OH)2
Li-ion
Anode: LiC6 (Li, Li15Si4)
Electrolyte salts:
  LiPF6, LiBF4, LiClO4
Cathodes:
  Li2TiO3 (LTO)
  LiCoO2 (LCO)
  LiFePO4 (LFP)
  LiMn2O4 (LMO)
  LiNiCoAlO2 (NCA)
  LiNiMnCoO2 (NMC)*

## Slide 4: Strong Li-ion demand increase
https://www.greentechmedia.com/articles/read/10-battery-gigafactories-are-now-in-progress-and-musk-may-add-4-more
https://www.visualcapitalist.com/battery-megafactory-forecast-1-twh-capacity-2028/

## Slide 5: Rising production, declining cost
https://www.economist.com/graphic-detail/2017/08/14/the-growth-of-lithium-ion-battery-power

## Slide 6: Li-ion
https://batteryuniversity.com/learn/article/types_of_lithium_ion
Li et al. Adv. Mater., 2018, 30, 1800561
DOI: 10.1002/adma.201800561

## Slide 7: Battery operation
Liu et al. Chem. Commun., 2011,47, 1384-1404
DOI: 10.1039/c0cc03158e
https://www.energy.gov/eere/articles/how-does-lithium-ion-battery-work

## Slide 8: Production Process
https://www.mpoweruk.com/battery_manufacturing.htm
https://electronics.howstuffworks.com/everyday-tech/lithium-ion-battery1.htm

## Slide 9: Materials sourcing: lithium
https://minerals.usgs.gov/minerals/pubs/commodity/lithium/mcs-2019-lithi.pdf
“The only lithium production in the United States was from a brine operation in Nevada.”
“Although lithium markets vary by location, global end-use markets are estimated as follows: batteries, 56%; ceramics and glass, 23%; lubricating greases, 6%;…Lithium consumption for batteries has increased significantly in recent years because rechargeable lithium batteries are used extensively in the growing market for portable electronic devices and increasingly are used in electric tools, electric vehicles, and grid storage applications.”
“Import Sources (2014–17): Argentina, 51%; Chile, 44%; China, 3%; Russia, 1%; and other, 1%.”

## Slide 10: Minerals sourcing: cobalt
https://minerals.usgs.gov/minerals/pubs/commodity/cobalt/mcs-2019-cobal.pdf
“About 46% of the cobalt consumed in the United States was used in superalloys, mainly in aircraft gas turbine engines;”
“Congo (Kinshasa) continued to be the world’s leading source of mined cobalt, supplying more than 60% of world cobalt mine production. China was the world’s leading producer of refined cobalt and has been a leading supplier of cobalt imports to the United States. China was the world’s leading consumer of cobalt, with more than 80% of its consumption being used by the rechargeable battery industry.”
Notes: 8% in cemented carbides for cutting and wear-resistant applications; 15% in various
other metallic applications; and 31% in a variety of chemical applications.
Import Sources (2014–17): Cobalt contained in metal, oxide, and salts: Norway, 18%; China, 12%; Japan, 12%;
Finland, 9%; and other, 49%.
The cobalt contents of lithium-ion batteries, the leading global use for cobalt, are expected to be
reduced rather than eliminated; nickel contents of lithium-ion batteries will increase as cobalt contents decrease.

## Slide 11: Materials recycling
Lithium: One domestic company has recycled lithium metal and lithium-ion batteries since 1992 at its facility in British Columbia, Canada. In 2015, the company began operating the first U.S. recycling facility for lithium-ion vehicle batteries in Lancaster, OH.
Cobalt: In 2018, cobalt contained in purchased scrap represented an estimated 29% of cobalt reported consumption.
Nickel: recycled nickel in all forms accounted for approximately 52% of apparent consumption.
https://minerals.usgs.gov/minerals/pubs/commodity/lithium/mcs-2019-lithi.pdf
https://minerals.usgs.gov/minerals/pubs/commodity/cobalt/mcs-2019-cobal.pdf
https://minerals.usgs.gov/minerals/pubs/commodity/nickel/mcs-2019-nicke.pdf

## Slide 12: Current battery recycling process
https://www.laboratory-journal.com/science/chemistry-physics/recycling-lithium-ion-batteries
Notes: Approximately 50% of spent lithium ion (Li-ion) battery assets are recovered and recycled in Europe, China, South Korea, and Japan. In contrast, less than 5% of all Li-ion battery assets are recycled in the US. While cobalt and lithium are thought to be the two most valuable metals found in Li-ion batteries (with consumption of both reportedly outpacing production in the past 5 years), other metals like iron, nickel, aluminum, and magnesium also have positive revenue implications when recycled. Still, the US lacks the domestic supply of both lithium and cobalt.

## Slide 13
“An increase in private‑sector domestic exploration, production, recycling, and reprocessing of critical minerals…will reduce our dependence on imports, preserve our leadership in technological innovation…”
“A “critical mineral” is a mineral identified… to be (i) a non-fuel mineral or mineral material essential to the economic and national security… (ii) the supply chain of which is vulnerable to disruption, and (iii) that serves an essential function in the manufacturing of a product”
https://www.whitehouse.gov/presidential-actions/presidential-executive-order-federal-strategy-ensure-secure-reliable-supplies-critical-minerals/
Executive Order 13817

## Slide 14
“These efforts aim to reclaim and recycle critical materials (e.g., cobalt and lithium) from lithium-based battery technology”
“The goal…to profitably capture 90% of all lithium based battery technologies…Currently…recycled at a rate of less than 5%.” “award cash prizes totaling $5.5 million”
A direct cathode recycling focus will develop recycling…without the need for costly reprocessing;
Create technologies that cost effectively recycle other battery materials
Design for recycling will develop new battery designs optimized
Modeling and analysis tools

## Slide 15
https://americanmadechallenges.org/batteryrecycling/

## Slide 17: Pyrometallurgical processing
Al-Thyabat et al., Minerals Engineering, 2013, 45, 4-17
DOI: 10.1016/j.mineng.2012.12.005

## Slide 18: Hydrometallurgical processing
N. Vieceli et al., Waste Management 71 (2018) 350–361
DOI 10.1016/j.wasman.2017.09.032
Wang et al., J. Sustain. Metall. 2015, 1, 168–178
DOI 10.1007/s40831-015-0016-6

## Slide 19: Direct cathode recovery
Huang et al., Journal of Power Sources 399 (2018) 274–286
DOI: 10.1016/j.jpowsour.2018.07.116

## Slide 20
Deep eutectic solvent (DES) composed of choline chloride and ethylene glycol (ChCl:EG)
DOI: 10.1038/s41560-019-0368-4
Published April 1, 2019

## Slide 21
Ciez, Whitacre. Nature Sustainability, February2019, 2, 148–156
DOI: 10.1038/s41893-019-0222-5
“several battery recycling processes exist, the greenhouse gas emissions impacts and economic prospects of these processes differ”
“We compare three recycling processes: pyrometallurgical and hydrometallurgical recycling processes…and direct cathode recycling”
“While pyrometallurgical and hydrometallurgical processes do not significantly reduce life-cycle greenhouse gas emis- sions, direct cathode recycling has the potential to reduce emissions and be economically competitive. Recycling policies should incentivize battery collection and emissions reductions through energetically efficient recycling processes.”

## Slide 22
Ciez, Whitacre. Nature Sustainability, February2019, 2, 148–156
DOI: 10.1038/s41893-019-0222-5

## Slide 23
Ciez, Whitacre. Nature Sustainability, February2019, 2, 148–156
DOI: 10.1038/s41893-019-0222-5

## Slide 24: Questions to discuss
What are the bottlenecks in Li-ion battery recycling?
How could/should the public sector continue to address this topic?
How might the private sector be incentivized to invest in battery recycling?
What needs to happen to make direct recycling technically and economically feasible?

## Slide 25: Appendix: Li-ion element breakdown
https://www.rechargebatteries.org/wp-content/uploads/2018/05/RECHARGE-The-Batteries-Report-2018-April-18.pdf

## Slide 26: Appendix: Materials sourcing: nickel
https://minerals.usgs.gov/minerals/pubs/commodity/nickel/mcs-2019-nicke.pdf
“Approximately 47% of the primary nickel consumed went into stainless and alloy steel products, 41% into nonferrous alloys and superalloys, 7% into electroplating”
“Import Sources (2014–17): Nickel contained in ferronickel, metal, oxides, and salt: Canada, 41%; Norway, 11%;Australia, 8%; Russia, 8%; and other, 32%. Nickel-containing scrap, including nickel content of stainless steel scrap: Canada, 40%; Mexico, 28%; United Kingdom, 8%; and other, 24%."

## Slide 27: Appendix: Li-ion by chemistry
https://www.li-cycle.com/blog

## Slide 28: Appendix: CO2 emissions
US average (US)
low emitting grid, the Northwest Power Pool (NWPP)
higher-emitting grid, the ReliabilityFirst Corporation/Michigan (RFCM)

## Slide 29: Hydrometallurgical processing
N. Vieceli et al., Waste Management 71 (2018) 350–361
DOI 10.1016/j.wasman.2017.09.032

## Slide 30: Hydrometallurgical processing
https://www.researchgate.net/figure/Hydrometallurgical-model-for-recycling-lithium-battery-see-online-version-for-colours_fig1_308063762