## Slide 1: Porous Materials for Energy Applications
Mandy Liu
HEJC
10/11/2019

## Slide 2
What are Porous Materials?
Broadly define: porous materials are materials with internal voids
1 cm
Surface area: 6 cm2
1 cm
1 nm
Surface area: 6000 m2

## Slide 3: Why Porous Materials?
High surface area: gas adsorption & storage
Gas molecules
H2 storage
CH4 storage
CO2 sequestration
H2O adsorption (heat pump)

## Slide 4: Why Porous Materials?
Pore size/chemistry: physical & chemical separations/membrane technology
Conserve energy usage
Industrial energy consumption: 32770 TBtu/yr
Largest energy consumption sector, > 1/3 US energy use
22% of all in-plant energy use (4500 TBtu/yr) on separation technology
Harvest new energy sources
Uranium (nuclear energy source) mining from sea water (about 500 times more than land ores storage)
Materials for Separation Technologies: Energy and Emission Reduction Opportunities, US DOE
https://www.machinedesign.com/materials/uranium-extracted-seawater
Notes: Materials for Separation Technologies: Energy and Emission Reduction Opportunities, US DOE

## Slide 5: How to Generate Porosity?
Top-down approach
“extrinsic” porosity
Etching
(With acid/base)
Bottom-up approach
“intrinsic” porosity

## Slide 6: Characterization of Porous Materials
Electron microscopy
Macropore (>50 nm)
Gas adsorption
Meso (> 2 nm) + micropore
Crystal structure
Micropore (< 2 nm)
1,5 nm
http://www.atl.semtechsolutions.com/node/44/particle-pore-size-analysis
Mason, Oktawiec, Taylor, Hudson, Rodriguez, Bachman, Gonzalez, Cervellino, Guagliardi, Brown, Llewellyn, Masciocchi, Long, Nature, 2015, 527, 357
Mason, Veenstra, Long, Chem. Sci, 2014, 5, 32
Notes: http://www.atl.semtechsolutions.com/node/44/particle-pore-size-analysis

## Slide 7: Types of Porous Materials
Elemental/atomic
Activated carbon
Up to 3000 m2/g
Drinking water filtration
Fuel (H2/CH4) storage
Inorganic
Corning ”thirsty” glass
250 m2/g
Water/organic contaminants absorption
Zeolites
< 1000 m2/g
Aluminosilicate, ex: Na2Al2Si3O10·2H2O
Catalytic cracking for petroleum industry
Nuclear waste reprocessing
http://www.corningcn.com/docs/specialtymaterials/pisheets/Vycor%207930.pdf
Notes: http://www.corningcn.com/docs/specialtymaterials/pisheets/Vycor%207930.pdf

## Slide 8: Types of Porous Materials
Organic
Porous organic polymers (POPs)
Membrane applications
Gas permeability
Natural gas purification & carbon sequestration
Covalent organic frameworks (COFs)
Metal-organic
Metal-organic frameworks (MOFs)
Metal centers introduce new chemistry (selectivity/reactivity)
Composite materials
He, Benedetti, Lin, Liu, Zhao, Ye, Voorhis, Angelis, Swager, Smith, Adv. Mater., 2019, 31, 1807871
https://phys.org/news/2015-09-exploration-stable-crystalline-porous-covalent.html
Mason, Veenstra, Long, Chem. Sci, 2014, 5, 32

## Slide 9: Case 1: Gas Storage with MOFs
https://www.youtube.com/watch?v=QaKSekjAnqY
Limitations of metal hydride/ chemical hydrogen storage: higher operational temperature
larger environmental impact
Farha, Hupp & Snurr, Northwestern University,
https://www.energy.gov/eere/fuelcells/materials-based-hydrogen-storage
Mason, Veenstra, Long, Chem. Sci, 2014, 5, 32

## Slide 10: Case 1: Gas Storage with MOFs
Methane storage
2012 DOE goal: 350 cmSTP3cmadsorbent3 (v/v)
Activated carbon: 100– 170 v/v
Zeolites lower due to lower surface area
MOFs with open active site: up to 230 v/v
Higher level of chemical design enabled by MOFs
Mason, Veenstra, Long, Chem. Sci, 2014, 5, 32
Mason, Oktawiec, Taylor, Hudson, Rodriguez, Bachman, Gonzalez, Cervellino, Guagliardi, Brown, Llewellyn, Masciocchi, Long, Nature, 2015, 527, 357

## Slide 11: Case 2: Water-Adsorbing MOFs
Yaghi & Wang, UCB: water harvesting from desert
Uptake at low relative humidity (20% RH)
Desorption powered by the sun
Device cross section

## Slide 12: Case 2: Water-Adsorbing MOFs
Adsorption heat pump
MOF adsorb water -> system heats up -> desorb water -> system pressurized -> water condense & absorb heat (cooling) -> T drops -> MOF adsorb water again
https://warwick.ac.uk/fac/sci/eng/research/grouplist/sustainableenergy/heatpumps/adsorption/
Adsorbent
Cascade heat pump
Dinca, MIT
https://www.researchgate.net/figure/Simplified-Diagram-of-the-GHPWH-Absorption-Heat-Pump_fig2_320596506,
Rieth, Wright, Rao, Kim, LaPotin, Wang, Dinca, J. Am. Chem. Soc., 2018, 140, 17591
Notes: Absorb water, heat up (ambient), desorb, pressurized, condense, absorb heat, cool down (ambient), absorb again
Improve efficiency
https://www.researchgate.net/figure/Simplified-Diagram-of-the-GHPWH-Absorption-Heat-Pump_fig2_320596506

## Slide 13: Case 3: Chemical Separation
O-xylene
M-xylene
P-xylene
Ethylbenzene
Gonzalez; Kapelewsk; Bloch.; Milner; Reed.; Hudson; Mason; Barin; Brown; Long, J. Am. Chem. Soc. 2018, 140, 3412.

## Slide 14: Why not more MOFs in the industry?
Low processability
Nonuniformity (grain boundaries)
Undesirable mechanical property
  Fragile
  Brittle
Air/water/thermal stability
Cost (metal, synthetic)
Scalability
Better industrial future requires new chemistry & materials research

## Slide 15: Thank You! Questions?